## Slide 1
Erosion corrosion of HastelloyC-276 Piping in residue service
Presented by:
Vijaykumar Bhuva
Static Engineer, R&I

## Slide 2: CONTENTS
INTRODUCTION
HASTELLOY C-276
RESIDUE SYSTEM
INSPECTION FINDINGS
FAILURE ANALYSIS
DAMAGE MECHANISM
ENHANCEMENT ACTION
RESULTS SUMMARY

## Slide 3: INTRODUCTION
Piping handling hazardous Residue services
Any leakage- leading EHSS concerns, stoppage of unit
Piping material: Hastelloy-C276
Piping material having issue with corrosion, these Leading frequent leakages
Frequent leakages reported from Piping components in past
Detailed study had been conducted for frequent leakages

## Slide 4: RESIDUE SYSTEM
1” Min. Circ. line,
DT: 205 °C, OT: 105-115°C,
DP: 10 bar, OP: 6 bar
2” Discharge
FO
Residue Transfer Pump
Residue Vessel
Heavy Residue
H2SO4
(5-15%)
Acetic acid
Water
Other HC

## Slide 5: HASTELLOY C-276 MATERIAL
Hastelloy C-276
UNS N10276
Excellent corrosion resistant
Proven- Aggressive process

## Slide 6: INSPECTION FINDINGS
  Highest corrosion rate 0.60 mm/year
Severe Corrosion
Leakages
PMI

## Slide 7: FAILURE ANALYSIS- HYPOTHESIS
PMI Testing & MTC
Material as per speciation
Improper Welding-
QA/QC procedure
PWHT
Solution annealing procedure
Corrosion
Observed on similar service piping
Further Analysis Required
NON-SPEC. MATERIAL
WELDING ISSUE
CORROSION
EROSION CORROSION
Ruled out
Ruled out
Possible
Possible

## Slide 8: DAMAGE MECHANISM
Line Size 1”,
FO Has been removed
Erosion Corrosion
& Corrosion
Varying fluid viscosity
High Velocity
Specification: 40 CP
Actual range- 17 to 1667 CP
Chocking issue
LP and MP steam utilized for de-chocking
105-115°C
5-15% Sulfuric acid
Flushing practice
Operating Fluid

## Slide 9: DAMAGE MECHANISM
Operating window

## Slide 10: ENHANCEMENT ACTION
Resizing
(Design)
Resized from 1” to 2”
Involved Licenser for feasibility
Resizing calculation
  Velocity calculation
  Hydraulic calculation
  Proper FO size calculation
PWHT treatment
Solution annealing treatment for Hastelloy material to reduce corrosion
Improve Operation
Control Viscosity
Range of 20-80 CP by additional acetic acid for dilution
Flushing practice
Avoid steam flushing
Utilization of Hydrokinetic technique for cleaning
Material Upgradation
PTFE lined
1. Liner Failure
2. Electrical tracing limitation
3. Chocking of lines
Tantalum
1. Very Expensive
2. No Experience
3. Chances of Hydriding
Zirconium
1. Less Expensive
2. Proven Experience
Operating temperature reduction
X

## Slide 11: RESULTS SUMMARY
No erosion corrosion after Resizing with Zirconium
Improve integrity of piping system
Zero leakage goals have been achieved.
Note:
Special attention to be given for Acid service material selection while designing any plant equipment or piping
Only minor change in concentration, chemical composition or temperature will affect equipment material selection

## Slide 12
Thank You