## Slide 1
Preheaters Erosion Case Study
Troubleshooting, Analysis and Recommendations
Presented By: Kareem Khalil
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES

## Slide 2: Outline
Process Description
Equipment Design
2018 DBN Changes
Findings
Short Term Solution
HTRI Analysis
Long Term Recommendations

## Slide 3: Process description
Prior to entering the glycol reactor, the EO-water solution goes through four (4) pre-heaters in order to reach the desired temperature (90 C) of the reaction to convert all the EO to glycol. In the first stage pre-heater (E-2520A/B), the process goes through the tube side and gets heated by the hot condensate in the shell side coming from the sixth effect re-boiler condensate drum (V-2536) through the evaporator condensate pump (P-2535A/B).

## Slide 4: Exchanger datasheet
Item (Shell Side) | Value
Process | Condensate
Inlet Pressure | 392 kPa
Inlet Temperature | 120 C
Inlet Nozzle | 16 “ 300 #
Shell Material | CS
Corrosion Allowance | 6 mm

## Slide 5: Design details
Item | Value
Shell Material | SA-516 Gr 70
Shell Thickness | 24 mm
Nozzle Material | SA-105
Nozzle Neck Material | SA-106 Gr B
Nozzle Neck Thickness | 17 mm
Design Pressure | 27 barg
Design Temperature | 166 C
Joint Efficiency | 1.0
Insulation Thickness | 50 mm

## Slide 6: 2018 DBN
Observations of the changes before and after the DBN:
The pump design pressure was increased from 506.0 to 667.4 Kpa(g) which represents 32% increase in the discharge pressure.
The pump capacity increased from 775 M3/hr to 951.5 M3/hr which represents 22% increase in the discharge pressure.
Pump actual discharge flow increased by 75 T/hr which is 11.1% higher, comparing 125% and 140% plant load.
Pump actual discharge pressure increased from 480 kpa(g) to 790 Kpa(g) which is %65 higher, comparing 125% and 140% plant load.
No noticeable difference observed in the operating temperature.
Preliminary findings:
Higher flow (+11.1%) and higher pressure (+65%) in E-2520 shell side after the DBN are the major findings that could have increased E-2520 A/B erosion rate.
Before the DBN:
After the DBN:

## Slide 7: Trends (E-2520 Operating Parameters before and after dbn).
Chart: 2017/18 Run
Chart: 2019/20 Run

## Slide 8: Findings (Erosion observed at shell side)

## Slide 9: Findings (Erosion observed at shell side)

## Slide 10: Findings (Erosion observed at shell side)

## Slide 11: Findings (Erosion observed at shell side)

## Slide 12: Findings (Erosion observed at shell side)

## Slide 13: HTRI Load Comparison
Simulation by HTRI done in-house. Warning message: Shell entrance velocity exceeds critical velocity, indicating a probability of fluid elastic instability.
Calculations show that the exchanger is designed to a maximum of 85% of plant capacity.

## Slide 14: Recommendations
  Change the material for both exchangers shell inlet and outlet nozzles for (E-2520A&B) from carbon steel (SA516-70) to stainless steel (SA304).
  Remove the current impingement plate for both exchangers.
  Make the top first three (3) rows of the tubes for each exchanger as impingement rods.

## Slide 15: New datasheet
Item (Shell Side) | Changes
Process | Condensate
Inlet Pressure | 392 kPa
Inlet Temperature | 120 C
Inlet Nozzle | 18” 300#
Shell Material | SS
Corrosion Allowance | None

## Slide 16
Reach out.
THANK YOU
email
phone
Calle Cualquiera 123, Cualquier Lugar
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES