## Slide 1
Hydrogen Induced Cracking (HIC) of Low- and High-strength Alloys
Presented By:
Nausha Asrar, Ph.D
Fatma AlRadhi, Asma AlGhamdi and Abdurahman AlAnazi
WTIIRA, Saudi Water Authority
Al-Jubail, Kingdom of Saudi Arabia
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES

## Slide 2
Mechanism of Hydrogen Generation
Types of Hydrogen Assisted Cracking (HAC)
Mechanisms of HAC
Cases of Low- and High-strength Alloy HAC
Concluding Remarks
Topics
SURFACE OF PIPE EXPOSED TO H2S AND MOISTURE
HAIRLINE FRACTURE DUE TO H2 AND TENSILE STRESS
PIPE WALL
HARDNESS GREATER THAN 22 HRc
TENSILE STRESS
CATHODE (FeS)
MILLIONTHS
OF AN INCH
FeS

## Slide 3
Hydrogen Generation
Anodic reaction (Oxidation)
Fe  Fe++ + 2e-
Cathodic reaction (Reduction)
2H+ + 2e-  H2
Electrochemistry of Corrosion Reaction

## Slide 4
Hydrogen Generation
In aqueous environment hydrogen atoms are produced on a metal surface by a corrosion reaction, cathodic protection, electroplating, or acid pickling
Some H atoms form hydrogen gas molecule and escape as gas bubbles
Under certain conditions protons (H+) enters into the metal  Blistering, Hydrogen Assisted Cracking (HAC), Hydrogen Embrittlement (HE).
Sulfide ions, phosphorus and arsenic compounds retard the formation of H2 molecule at the metal surface, and increase the entry of hydrogen into the metal  Sulfide Stress Cracking (SSC).

## Slide 5
Hydrogen Blistering
Hydrogen Embrittelemnt (HE)
Hydrogen Induced Stress Cracking (HISC)
Stress Oriented Hydrogen Induced Cracking (SOHIC)
Hydrogen Induced Cracking (HIC)
Sulfide Stress Cracking (SSC)
Sulfide Stress Corrosion Cracking (SSC)
Hydrogen Assisted Cracking (HAC)
All the same or different ?

## Slide 6
Hydrogen Assisted Cracking (HAC)
Hydrogen blistering
  Hydrogen enters into low-strength ductile steels
  Macroscopic defects (inclusions, lamination etc.) in the steel provide space for H2 formation  pressure build up  Blistering
  Hydrogen may be formed during cleaning, plating, corrosion etc.
Hydrogen Embrittlement (HE)
  Influence of sustained load + H-charging  Material embrittlement
  Internal HE - Hydrogen enters molten metal
  Environmental HE – Absorbed by solid metal
  W/o stress - blistering, internal cracking, hydride formation, reduced ductility
  With stress - H interacts with the metal  subcritical crack growth  Fracture
Blistering
Hydrogen Embrittlement

## Slide 7
Hydrogen Assisted Cracking (HAC)
Sulfide Stress Cracking (SSC)
  Combined action of stress and corrosion in presence of wet H2S environment
  Spontaneous brittle failures of steels and other high-strength alloys
  Also called as sulfide cracking, sulfide corrosion cracking, sulfide stress corrosion cracking
  Hydrogen Assisted/Induced Cracking (HAC or HIC)
    Absence of corrosion reaction (Polarized cathodically)  HAC
    In presence of corrosion (Polarized anodically)  Hydrogen Assisted Stress-corrosion Cracking (HASC) or HISC

## Slide 8
Mechanism of HAC
The exact mechanism that causes hydrogen embrittlement in a metal are not clearly understood. There are currently three main contending theories: HELP, HEDE, and AIDE.
HELP – Hydrogen Enhanced Localized Plasticity
  Resistance to dislocation movement (one of the main strengthening mechanisms in metals) is reduced due to localized softening that occurs when solute hydrogen collects around mobile dislocations
  Lower stress required to move the dislocation (causing slip)

## Slide 9
Mechanism of HAC
HEDE – Hydrogen-Enhanced Decohesion
  In the HEDE mechanism, the hydrogen atoms accumulate within certain regions of the crystal lattice and reduce the cohesive energy of the metal matrix or at specific interfaces. This allows tensile separation (decohesion) to occur rather than the normal slip.
The weakening of the bonds is attributed to a decrease in the electron-charge density between metal-to-metal atoms as a result of the hydrogen.

## Slide 10
Mechanism of HAC
AIDE – Adsorption-Induced Dislocation Emission
  HELP + HEDE theories.
  It postulates that hydrogen at the crack tip weakens the metal-to-metal bonds as described for the HEDE theory, but the actual crack growth is the result of localized dislocation slip as described by the HELP theory.
It is currently believed that the hydrogen ion is electrostatically charged directly into the cathode without first forming an adsorbed hydrogen atom.
Charging of the hydrogen into the metal is extremely powerful faradaic process and not just a diffusion process based upon the concentration differential of hydrogen at the sea water/metal interface.

## Slide 11
Hydrogen Charging and HAC
HAC depends on:
  How much hydrogen is charged
  The mobility of the hydrogen within the metal
  Where the hydrogen accumulates within the metal
How much hydrogen is charged into a metal depends on cathodic charge/protection
The mobility of the hydrogen and where it accumulates depends on the microstructure of the metal
BCC (ferritic) materials – High diffusivity low hydrogen adsorption capacity  More susceptible to HAC
FCC (austenitic) materials – Low diffusivity high hydrogen adsorption capacity  Less susceptible to HAC

## Slide 12
Hydrogen Charging and HAC
Susceptibility of a given metal to HAC increases with;
  increasing strength
  inclusion content, and
  cold work
These either provide traps in the microstructure for hydrogen to accumulate at or facilitate diffusion of hydrogen into the metal
The risk of hydrogen induced stress cracking (HISC) increases in most metals as the stress (residual and/or applied) increases

## Slide 13
Important Info about HAC
Low-alloy steels are most likely to crack (SSC) near ambient temperature
Temperature Effect on SSC
The stronger the steel, the less H2S it can take, or the more cracking susceptible it becomes
Strength Effect on SSC
Higher strength grades can be used at higher temperatures
Temperature and Strength vs SSC

## Slide 14
HAC Cases of Low- and High-strength Alloys

## Slide 15
Hydrogen Embrittlement of a Stainless Steel Shaft
O&G drilling tool failure
SlimPulse main shaft transfers rotary motion from the motor to the impeller and restrictor
Failed during straightening for re-coating
Material - Stainless steel 17-4PH (H900 grade, Hardness HRc 35 - 41) - Alloy 17-4PH (UNS S17400), Type 630, is a chromium-nickel-copper precipitation-hardening martensitic stainless steel with an addition of niobium. 17-4PH combines high strength and hardness with good corrosion resistance.
SEM fractography
Isolated intergranular cracking
Brittle fracture via quasi-cleavage

## Slide 16
Hydrogen Embrittlement of a Stainless Steel Shaft
Material embrittled due to hydrogen diffusion
Bending load applied during the re-straightening process is likely to facilitate the propagation of pre-existing hydrogen induced cracking (HIC)
Presence of metal sulfides at the fracture surface – possible exposure to H2S containing mud
High hardness (HRc > 33) material – Non-NACE compliant
For reliable operation - material must be compatible to the drilling fluid
EDS analysis identified S and Cl on fractured surface

## Slide 17
HAC of Carbon Steel Boiler Tube
Water-wall or riser tubes of the steam boiler of MSF desalination plant ruptured.
Boiler is a dynamic balance between heat flow from the combustion of a suitable fuel and steam formation. Seel tube is "heated" by the flame and simultaneously "cooled" by the fluid (steam, water or a mixture of steam and water) flow.
Material - Medium carbon steel ASTM A178 / SA178C.
Thick lip cracking, corrosion on the internal side, decarburized microstructure with intergranular cracking.
Tube of boiler No. 65
a) Tube of boiler No. 65
Microstructure showing typical ferrite and pearlite phases with signs of decarburization and grain growth.
Thick lip random rupture of the boiler tube
Corrosion on internal surface

## Slide 18
HAC of Carbon Steel Boiler Tube
SEM picture showing sites of intergranular
cracking (arrow marked)
Metallograph showing
intergranular cracking
When contaminants lower the boiler water pH sufficiently, the acid attack of the steel generates hydrogen.
Hydrogen diffuses into the metal and reacts with the carbon content to form methane gas. The large size and quantity of methane molecules will generate excessive pressure within the metal structure and result in micro-crack formation, causing a violent and sudden metal rupture.
Grain growth, thick lip fracture and random cracking feature seem the signs of hydrogen induced cracking mechanism.
Intensity and distribution of gas pressure is not uniform along the metal surface, resulting in the occurrence of failure at areas that can no longer withstand the internal pressure.
Ruptured sections usually retain their original thickness.

## Slide 19
Concluding Remarks
NACE MR0175 compliant materials are resistant to SSC not to wet H2S corrosion
Hydrogen charging depends on:
  How much hydrogen is charged
  The mobility of the hydrogen within the metal
  Where the hydrogen accumulates within the metal
Susceptibility of a given metal to HAC increases with;
  Increasing strength
  Inclusion content
  Cold work

## Slide 20
Concluding Remarks
Compressive stress on ID surface can lower the initiation of cracking
In case boiler tubes presence of hard and adherent deposits facilitate the build up of hydrogen pressure within the deposit layer to penetrate the steel tube wall. Hydrogen reacts with the carbon content to form large molecules of methane gas, which generate excessive pressure within the metal structure and result in crack formation, causing a violent and sudden metal rupture.
Inspection and cleaning of the boiler tube per the design requirement and maintenance of the specified chemistry of feed water are the remedial measures to avoid HAC of boiler tubes.

## Slide 21
Reach out.
THANK YOU
Email: nasrar@swcc.gov.sa
Phone: 056-389-1865
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES