## Slide 1
SCC of SS 321H pipe in high temperature service in Ethylene Cracker furnace
3rd Sept 2024
Presented By:
Karan Potnis
Sr. Static Engineer
Bachelor in Mech Production
17 years experience
Specialized in fired equipment
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES

## Slide 2
Seven Pyro crack 1-1 furnaces
Six furnaces in operation & one standby
96 passes/96 LQE arranged in 8 modules with 12 outlet passes in each
192 inlet tubes per furnace
FURNACE DESIGN
FURNACE
PQE/TLE
SQE

## Slide 3
DAMAGE MECHANISMS
01
02
Creep
Carburization
03
06
04
Nitridation
Oxidation
Erosion in
Steam & BFW
Refractory
degradation
PTASCC
CLSCC
08
07
BFW corrosion
Sulfidation
09
10
Carbonic acid
corrosion
Flue gas dew
point corrosion
Radiant & HTC 2 coils
Associated piping
Radiant & Convection
Radiant & Convection coils
Convection & Casing

## Slide 4: SCHEMATIC OF INLET PIPE & PG CONNECTION
Pipe size | Material | Process | Oper. temp | Oper. press | Qty per furnace
2 inch (inlet pipe) | SS 321H | C2 C3/C4 | 649 °C | 1.83 barG | 192 (24x8)
¾ inch (PG line) | SS 321H | C2 C3/C4 | 649 °C (Insulated) Ambient (non insulated) | 1.83 barG | 192 (24x8)
¼ inch (analyzer tube) | SS 321H | C2 C3/C4 | Ambient | 1.83 barG | 8 (8x1)
Grating
Pressure Guage
Indication of choking
Consideration for tube replacement
¼” PT line
PG
Furnace roof
Spring hanger
Header
2 “ Inlet pipe
¾ “ PG pipe
Laval nozzle
2 “ Inlet tube
Spring Support
Inlet radiant tube
Constant spring hanger
PG line fixed with U clamps

## Slide 5: FAILURE LOCATION
Crack on parent material
Crack on weld joint
Closer view shows crack on weld toe
PG
Furnace roof
Spring hanger
Header
¼” PT line
Spring Support

## Slide 6: FAILURE ANALYSIS
Visual
Low magnification
DPT
LAB TESTING
Tensile
Hardness
Micro
Macro
SEM
EDS
Chemical
Through crack
Meet spec
Rough surface
Sulfur on ID
Chloride on OD
Through crack
Intergranular crack
Within limit
Seamless pipe
Satisfactory
IGC from inside
OD corrosion
OD crack
ID crack
OD corrosion
ID crack
DPT on OD
DPT on ID

## Slide 7: MICROSTRUCTURE ANALYSIS
OD corrosion
ID intergranular cracking
along with grain dropping
SEM showing intergranular cracking on ID
Carbide precipitation on grain boundary
Typical behavior of Polythionic acid stress corrosion cracking
ICG with grain dropping
Sulfur is present is stream with steam
Possible due to chloride from insulation
OD corrosion at insulation opening
Carbide precipitation at grain boundary
Sensitized steel operating at 650 degC

## Slide 8: STRESS ANALYSIS
Tube moves downward whereas the PG is not free to move
Stress point identified on the PG connection to 2” pipe
Rigidity increased as four PG pipes connected together
Overhung creates load on the weld joint
PG
Stress point
Rigid support
Furnace roof
Spring hanger
¼” PT line
Spring Support
Header
Constant spring hanger
PG line fixed with U clamps

## Slide 9: THERMOGRAPHY ASSESSMENT
Temperature drops from 600 degC to 120 degC
Sulfur condensation in PG pipe
Temperature drops from 125 degC to ambient
High thermal gradient

## Slide 10: CRACK ASSESSMENT FAULT TREE
PG line cracking
Weld joint crack
Parent metal crack
SCC
Internal
(PTASCC)
External
(CLSCC)
Stress
Inadequate support
Tube additional expansion
Primary cause of failure
PTASCC - Polythionic acid stress corrosion cracking
CLSCC – Chloride stress corrosion cracking
Contributing cause of failure
PASCC: (Polythionic acid stress corrosion cracking)
API 571:
Intergranular SCC in sensitized austenitic stainless steels and some Ni alloys
Sulfide scale due to air and moisture creates sulfur acids causing PTA SCC.
Occurs during shutdowns or start-ups.
Assessment:
Sulfur in DMDS injection required for pre-sulfiding of the radiant coils.
Crack at the insulation opening location where temperature drops to ambient & condenses sulfur.
Stress due to the rigid system from improper supports.
Pipe material (SS321H) not stabilized which makes it more susceptible to PASCC.
CLSCC: (Chloride stress corrosion cracking)
API 571:
Surface cracking of 300 series SS and some nickel-based alloys under the combined action of tensile stress, temperature, and an aqueous chloride environment.
Temperature: 60°C to 205°C
Wet insulation
Assessment:
Chloride is present insulation.
Stress due to the rigid system from improper supports.
Moisture from ambient conditions during summer.

## Slide 11: PARENT MATERIAL CRACKING
Parent metal crack
SCC
PASCC
Inadequate support
CLSCC
Chloride from Insulation
Moisture from atmosphere
Pipe not insulated completely
Tube & PG pipe connected together
Nonfunctional spring hanger
Not designed for
Coke/HSSB/Decoking
4 tubes connected to one hanger
Design deficiency
Pipe not stabilized
Not in specification
Sulfur condensation
Insufficient insulation
Moisture
Shutdown/
Maintenance/
steam condensate
Primary cause of failure
PASCC - Polythionic acid stress corrosion cracking
CLSCC – Chloride stress corrosion cracking
Aluminum foil installed
Contributing cause of failure
Control measures implemented

## Slide 12: WELD JOINT CRACKING
Weld joint crack
Stress
Thermal shock
During trips/SD
Inadequate support
Residual
Welding
Nonfunctional spring hanger
Not designed for
Coke/HSSB/Decoking
Tube additional expansion
Tube overheating
Overweight
Tube choking
Tube choking
Impurities in recycle feed
PQE with hard coke
No PM for cleaning
4 tubes connected to one hanger
Tube & PG pipe connected together
Design deficiency
Flame impingement
Improper burner management
No PM for cleaning
Operational awareness
Primary cause of failure
Contributing cause of failure

## Slide 13: CONCLUSION
Inadequate
PG support
Stress analysis
Design modification
Nonfunctional tube hangers
Stress analysis
Pipe not stabilized
Tube additional expansion
Design modification
Change spec to include stabilization treatment
Reduce tube choking
Burner management
Recycle feed impurity
PQE cleaning
Cleaning PM
Operation monitoring
Site modification
Replace all pipes with stabilized grade
New replacement with stabilize grade
Shift PG
Loosen U clamps
PRIMARY CAUSE
CONTIBUTING CAUSES

## Slide 14: OPTION - 1 (Shift PG on top of vertical line)
Benefits
Shortcoming
Overhung stress elimination
  Conclusion
Will eliminate the failure probability
  No accessibility for monitoring & replacement
  New grating will be required
  Operator exposed to high temperature area
  Not feasible
PG
Furnace roof
Spring hanger
Header
2 “ Inlet pipe
¾ “ PG pipe
Laval nozzle
2 “ Inlet tube
PG
Spring Support
Current position
Proposed position

## Slide 15: OPTION – 2 (Shift the vertical line closer to grating & place PG on top of it)
Benefits
Shortcoming
  Overhung stress reduction
  Conclusion
  Requires replacement of inlet pipes
  Not feasible
  Will reduce the failure probability
  Accessibility for replacement is a concern
PG
Furnace roof
Spring hanger
Header
2 “ Inlet pipe
¾ “ PG pipe
Laval nozzle
2 “ Inlet tube
PG
Grating
Spring Support
Current position
Proposed position

## Slide 16: OPTION – 3 (Loosen U clamps)
Sketch only for understanding purpose
3 – Support plate
4 – PTFE sheet
5 – U clamp
6 – Not available on site
Benefits
Shortcoming
Free movement will minimize the stresses on the socket weld joint
  Conclusion
  Weld joint stress on the socket joint still exist but will be reduced
  Selected option
Immediate solution without major modifications
  Verified with Spring Support consultant
Space available for movement
Original - Rigid
Modified - Flexible

## Slide 17: OUTPUT & PATHFORWARD
Monitor change
Replace affected pipe
Stress analysis
Support modification
2022:Monitoring
2023:Analysis
Leak tracking
Solution
2 yrs.:21 leaks
1 yr.: Zero leak
01
02
03
04
Analysis & solution
Implementation & monitoring
Improved integrity & safety
Cost saving
Path forward
Output

## Slide 18: TAKEAWAY: SIMPLE IS BETTER
COMPLEX
01
02
03
OPT 1
OPT 3
OPT 3 – LOOSEN CLAMP
OPT 2
SIMPLE

## Slide 19
Reach out.
potniskk@tasnee.com
+966 (13) 359 9317
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES