## Slide 1
Presenter:
Dr Zia Chaudhary
Engineering Manager
D.Phill (Oxon), MSc, BSc, FICorr,
Corrosion Specialist (AMPP), CP Specialist (ICorr L4)
Corrosion Protection of Reinforced Concrete Structures with
Galvanic Surface Anode System:
(An effective and Long-term Performance Case History)

## Slide 2
Solutions that integrate products, engineering, and construction
Forensics & Engineering services
State of the art construction products
Specialty contracting
Notes:   There are three companies that make up Structural Group.
  We provide products and a broad ranger of engineering support services through Structural Technologies.
  And industry leading comprehensive specialty repair and new construction services through our two contracting companies, STRUCTURAL and PULLMAN.
  By combining these capabilities we offer our customers comprehensive turnkey solutions that integrate products, engineering support and contracting.

## Slide 3
Contents
An Overview of Corrosion of Reinforcing Steel
Cathodic Corrosion Protection
Galvanic Cathodic Protection of Steel in Concrete
  Description and Components of Surface Anode System (SAS)
  SAS Field Installations and System Performance
Conclusions

## Slide 4: Corrosion of Steel Reinforcement

## Slide 5: Passivation of Steel in New Concrete
High pH environment creates passivation layer

## Slide 6
Cl
Cl
Cl
Cl
Cl
Cl
CO2
CO2
CO2
CO2
CO2
CO2
Pitting Corrosion
PASSIVE FILM
pH>13
ELECTROLYTE
REINFORCEMENT
Cover
Steel
General Corrosion

## Slide 7: Volume of Iron & Reaction Products
Fe
FeO
Fe(OH)2
Fe3O4
Fe2O3
Fe(OH)3
Fe(OH)3.3H2O

## Slide 8: CORROSION PRODUCTS CRACK CONCRETE
The corrosion products
are more than 6 times the
volume of the steel consumed
Hydrated
ferric oxide
(rust)

## Slide 9: Cathodic Corrosion Protection of Steel Reinforcement

## Slide 10: Cathodic Protection
Cathodic Protection - the polarization of all noble potential areas (cathodes) to the most active potential (anodes) on the metal surface
Cathodic protection is achieved by making the structure the cathode of a direct current circuit.
Proven method in arresting corrosion of steel in chloride contaminated structures
Two Types:
  Galvanic Cathodic Protection Systems
  Impressed Current Cathodic Protection Systems
Polarization of a Structure

## Slide 11
Ch.3
Galvanic Cathodic Protection of Steel in Concrete Using:
Surface Anode System (SAS)
SAS Description & Components
Field Installations and System Performance

## Slide 12: Galvanic Surface Anode System (SAS) Working Principle

## Slide 13: Galvanic Surface Anode System (ZSAS) Components & Circuit
Zinc Mesh Anode:
Zinc mesh (2 to 4 Kg/m2) embedded in proprietary solid matrix.
Binder Matrix:
Formed by hardening of the shrinkage reduced embedding zinc activating cement (SEZAC) containing Tecto-Aluminosilicate-Cement (TASC).
Galvanic Connection
An electrical (cable) connection between steel and zinc anode, electrical current flow.
Concrete (Pore Water)
An electrolyte that conduct ionic current between steel and zinc anode.
Monitoring Probes
Embedded in concrete close to steel to evaluate galvanic system performance
Monitoring Probe

## Slide 14: Galvanic Surface Anode System (ZSAS) Components & Circuit

## Slide 15: Galvanic Surface Anode System (ZSAS) SEZAC Binder Matrix: Properties
Maintain an optimum electrolytic contact between the zinc anode and concrete overlay.
Maintain durable galvanic activity of zinc anode for long-term performance.
Prevent self-passivation of the zinc anode.
Assure high and durable adhesion towards the concrete overlay, >1.5 Mpa.
High electrolytic conductivity, specific resistance at 75% RH, <90 ohm.m
Provide enough space for anodic products formed
Suitable for pre-stressed concrete elements

## Slide 16: Galvanic Surface Anode System (ZSAS) Components: Macro-cell Sensor

## Slide 17: Galvanic Surface Anode System (ZSAS) Components: Macro-cell Sensor
Combined Reinforced Steel Corrosion – Concrete Temperature Sensor designed for monitoring Galvanic Protection Efficiency
Designed for monitoring cathodic protection (ICCP) and galvanic protection efficiency
  Monitor and measure local corrosion currents
  Monitor and measure concrete temperature
  Positive currents signify cathodic protection
  Negative currents signify corrosion current

## Slide 18: SAS Field Installations / Performance

## Slide 19
ALPLGRABEN BRIDGE, STYRIA, AUSTRIA: 11 Years of Galvanic Protection by SAS

## Slide 20
ALPLGRABEN BRIDGE, STYRIA, AUSTRIA: 11 Years of Galvanic Protection by SAS
Chloride contents of 4 to 5.6% by wt of cement was recorded in frequently wetted areas, and 0.5 to 0.9% in less wet areas.
System was installed / commissioned in Sept. 2007 and refurbished in July/August 2012 (zinc mesh was replaced on 1 m2, a cover coat applied) and restarted on 10 August 2012
Galvanic current in relation to macrocell currents indicating efficiency of galvanic corrosion protection

## Slide 21
HUBERTUS VIADUCT, DEN HAAG SAS installed on Beams of Hubertus Viaduct in 2008.

## Slide 22
HUBERTUS VIADUCT, DEN HAAG SAS installed on Beams of Hubertus Viaduct in 2008.

## Slide 23
HUBERTUS VIADUCT, DEN HAAG SAS installed on Beams of Hubertus Viaduct in 2008.

## Slide 24
HUBERTUS VIADUCT, DEN HAAG SAS Performance: Depolarization Test Data..

## Slide 25
PARKING DECK IN SAAS FEE, SWITZERLAND SAS installed on Parking Deck Slab in 2011.

## Slide 26
PARKING DECK IN SAAS FEE, SWITZERLAND SAS Depolarization Test Data Recorded in 2016.
SAAS FEE Car Parking Deck was built in 1979/80 and extended in 1981/82, with a total of 60,000 m2 of parking area.
The decks are reinforced with unbonded Post-Tensioned Tendons concrete.
Chloride contents of 0.5 – 3.0% by wt. of cement were recorded in deck slab ((source: Deicing Salt).
SAS was installed over deck slab in 2011 and coated with waterproofing and wearing surface of solid epoxy and covered with high abrasion resistant sealcoat.
SAS is in operation since 2011 and meeting the specified depolarization criterion.

## Slide 27
ALPINE TUNNEL ENTRANCE, STYRIAN ALPS SAS installed on Retaining Walls in 2018.

## Slide 28
ALPINE TUNNEL ENTRANCE, STYRIAN ALPS SAS Monitoring Using Macro-Cell Sensors
Retaining walls at tunnel entrance are exposed to very high thaw deicing salt loads.
Impact of salt exposure is intensified by wind channel effect.
Chloride contents of 1.6 – 6.0% by wt. of cement were recorded in R. Walls.
SAS was installed over Walls in 2017 and coated with epoxy coating (Sikagard-332) and topped dirt repellent protective coating (Sikagard-260).
ERE-20 reference cells and Macro-cell sensors were installed to monitor the SAS performance in protecting reinforcing steel from corrosion.

## Slide 29
ALPINE TUNNEL ENTRANCE, STYRIAN ALPS SAS Performance: Depolarization Test Data

## Slide 30
ALPINE TUNNEL ENTRANCE, STYRIAN ALPS SAS Performance: Depolarization Test Data

## Slide 31: Galvanic Surface Anode System (SAS) Field Samples Indicate Chloride Movement towards Zn Anode

## Slide 32: Galvanic Surface Anode System (SAS) Field Samples Indicate Chloride Extraction
Chlorides migrate towards the zinc-anode during the CP operation and are immobilized as zinc-hydroxide-chloride, a natural mineral Simonkolleite

## Slide 33
CONCLUSIONS
The galvanic protection afforded by SAS to the steel reinforcement is uniform, reliable, and long lasting.
No indication of passivation of zinc over an operational period of > 12 years
Expected service life of SAS with 2 to 4 Kg Zinc/m2 of steel is 20 - 30 years.
From a mean galvanic current of 3.6 mA/m2, one would expect a service life of 30-36 years.
Strong indication for chloride extraction and immobilization into SAS, coated with a water impermeable membrane
The SAS allows reliable protection and rehabilitation of RC structures under conditions ranging from alpine (low temperature, very dry periods) to marine environment (high temperature, high humidity, high chloride).

## Slide 34
Thank You!