## Slide 1
Jubcor Presentation
Adding Value Through Chemistry
Presented By: Muhammad Nawaz Hussian
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES

## Slide 2: PTA-SCC in Pre Heater coil
POLYTHENIC ACID STRESS CORROSION CRACKING

## Slide 3: TABLE OF CONTENT
Introduction to Farabi
Background of Process
Problem Statement
Investigation
Results of Inspection
Root Cause
Recommendations
Discussion

## Slide 4: Farabi Petrochemicals
Farabi Petrochemicals Group, located in the Kingdom of Saudi Arabia (KSA) is a global major in Linear Alkyl Benzene (LAB) & N-Paraffin business.
Farabi Group Comprises of Farabi Petrochemicals company (FPC), Farabi Yanbu Petrochemicals Company (FYPC), Farabi Downstream company (FDC), HADAF International Energy Company (HADAF) and Farabi Marketing company (FMC), located at Jubail and Yanbu Industrial cities of KSA.
Farabi today operates two world scale Normal Paraffin plants, and 3 world scale LAB plants, in addition to its specialty oils and specialty chemicals plants at Yanbu & Jubail. Farabi is the largest N-Paraffin and the second largest LAB Producer in the world today.
With the Commissioning of its new complexes at Yanbu & Jubail in 2020, Farabi today has a broad portfolio of around 1 million tons per year of Petrochemical intermediates and Specialty Surfactants.

## Slide 5: Background of process

## Slide 6: Background of process

## Slide 7: Background of Process
Furnace Design & Operating Parameter
Material: SA 312 TP 310 S
Diameter: 89 mm
Thickness: 4.5 mm
Pressure: 3 bar
Temperature: 780 C
Process Fluid: Hydrocarbons

## Slide 8: Background of process

## Slide 9: Background of Process
Material: SA 312 TP 310 S
Diameter: 133 mm /89 mm
Thickness: 4.5 mm
Pressure: 3 bar/ 1 bar
Temperature: 600 C/ 800
Process Fluid: Hydrocarbons

## Slide 10
Problem Statement
Found Cracks during start up
Location of cracks: On bellow/On welds of Bellow to pipe

## Slide 11
Problem Statement

## Slide 12
Investigation
Visual
Dimensional
Metallography
SEM and EDS analysis
Chemical Analysis
Hardness testing

## Slide 13
Results of Inspection
Cracking
Sensitization

## Slide 14
Results of Inspection

## Slide 15
Results of Inspection

## Slide 16
Root Cause

## Slide 17
POLYTHIONOIC ACID STRESS CORROSION CRACKING

## Slide 18: Mitigations and their Results???
Metallurgy
Austenitic Stainless steel
Solution Annealing
Nitrogen Purging
Mitigation
Dry Air Purging
Alkaline washing
Stabilization Heat Tretmen

## Slide 19: Questions???

## Slide 20
Reach out.
THANK YOU
hussainmn@farabipc.com
+966133565874
Calle Cualquiera 123, Cualquier Lugar
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES